## Slide 1: Multidimensional Strong PUF based on multifunctional thin films
Benjamin Malthiery1,2 (ORCID 0000-0002-4299-4467), Estelle Wagner1 (0000-0003-4837-483X),
Philippe Elbaz-Vincent2 (0000-0002-8629-3021), Giacomo Benvenuti1 (0000-0002-8369-636X)
1. 3D-Oxides SAS, 41 rue Henri Fabre, F-01630 Saint-Genis-Pouilly, France
2. Univ. Grenoble Alpes, CNRS, IF, 38000 Grenoble, France
Journées C2 2023 Oct. 15-20, 2023 Najac (France)

## Slide 2: Outline
Introduction
Thesis work
  Objectives
  Experimental results
Outlook

## Slide 3: I. Introduction
Need: combat counterfeiting and usurpation at lower cost
  Financial losses
  Deteriorated brand image
  Security & Public health problem
  Data exposed to a malicious actor
Context: IoT growth and process automatization
Concept: Applying biometrics to objects to provide reliable IDs at lower cost
CC BY-SA 3.0 DangApricot (rotated & cropped)

## Slide 4: Conceptual definition
Physical Unclonable Function (PUF) [1]
Dimensions
Select challenges
Interrogate PUF instance
Process responses
Process
…
Challenge
PUF
A
PUF
B
PUF
Xi
≠
≠
Instances axis  Uniqueness
Challenges axis
Responses axis
Time
Reliability
Randomness
 CRPs

## Slide 5: Use-cases and examples 1/2
Optical PUF & Authentication
  Authors: Pappu et al. (2002) [2]
  Challenge: Relative position of the laser beam
  Response: Speckle pattern
Laser
PUF
Camera
Response
Enrolment
Store CRPs in DB
Interrogate
PUF instance
Check response
Process
Select challenges
from DB
 Accept OR Reject
⊕
=

## Slide 6: Use-cases and examples (2/2)
SRAM PUF & Cryptographic key generation
  Authors: Guajardo et al. (2007) [3]
  Challenge: Position of the SRAM element
  Response: Power up state
Power-up behavior of an SRAM cell [4][5]
Response
Challenge
Read power up state
Generate private seed & helper data
Derive public-private key pair
Process
Neglect unstable values
1111001110010000…
Power-up
Stable A=0
Stable A=1
Metastable

## Slide 7: II. Thesis work – Objectives
PUF advantages vs. Secure Elements:
  Contained cost
  Improved logistics by skipping key provisioning
Identified limitations:
  Reader cost
  Clonability (SRAM) and modelling possibility [6]
Project objective: Develop a new PUF design based on oxides thin films
  Increase capacity of diversification
  Miniaturized and integrated reader

## Slide 8: Our approach
Multifunctional oxides thin films
  Multi-values basis
  Multi-properties challenges
Theoretical challenge space:
  L: Number of distinguishable values
  Z: Number of stimuli/properties
  N: Number of points
Property: optical transmittance
Oxides thin films reflectivity at different wavelengths (L&Z)
Thin film dots’ thickness AFM measurement (N)
1 µm
142
0
5 mm
Thickness (nm)
Optical thickness
(A. U.)

## Slide 9: Experimental results – Macro PoC (1/2)
Non-linearity of transmittance Thickness gradient (112 nm to 584 nm)
Movement of the plate
Oscillations between 76% and 97%
Interference effects decreases with increasing thickness (diffusion losses)
50 measurements
Thickness (nm)
600
100
Transmittance (%)
95
80
Thin film on transparent substrate

## Slide 10: Experimental results – Macro PoC (2/2)
Chart: Index of point
M1 | 80.9804 | 89.7971 | 92.4453 | 78.452 | 78.1502 | 81.1498 | 79.0065 | 82.5878 | 93.7969 | 95.8195 | 80.534 | 87.23 | 83.9785 | 79.7582 | 90.0553 | 80.7243 | 90.3005 | 88.8279 | 92.7599 | 82.4887 | 87.9872 | 82.0609 | 79.686 | 97.6948 | 83.1888 | 87.2738 | 85.0851 | 83.5204 | 95.131 | 88.2761 | 74.5637 | 82.1998 | 82.9058 | 96.186 | 86.8145 | 100.0633 | 76.5197 | 83.1478 | 83.1882 | 90.2914 | 77.9882 | 88.8548 | 88.8963 | 93.9036 | 82.5836 | 78.5217 | 84.9428 | 89.946 | 94.5362 | 80.2103 | 87.6306 | 77.8558 | 91.8251 | 94.7258 | 82.3941 | 77.9589
M2 | 80.5326 | 92.8777 | 96.5652 | 83.5933 | 78.6181 | 84.106 | 85.5294 | 83.8005 | 94.0009 | 97.3853 | 80.3741 | 88.5399 | 86.6954 | 85.7503 | 93.0141 | 81.0353 | 91.8927 | 90.9808 | 95.2551 | 82.5661 | 88.7615 | 80.8615 | 80.8102 | 98.1488 | 84.2688 | 87.231 | 85.9447 | 84.1308 | 94.2847 | 89.2341 | 74.6315 | 83.1499 | 84.7639 | 95.6979 | 88.2945 | 102.0203 | 77.6386 | 85.7821 | 85.8711 | 93.6554 | 78.5804 | 91.2964 | 92.7628 | 94.5726 | 84.4568 | 80.6211 | 89.1083 | 92.8387 | 95.6358 | 81.5907 | 89.1366 | 79.758 | 96.4219 | 95.8986 | 81.982 | 79.0609
M3 | 80.4102 | 89.38 | 92.6233 | 79.3466 | 77.416 | 81.4919 | 80.153 | 81.5711 | 93.2965 | 95.2316 | 79.27 | 86.5433 | 84.3186 | 80.3627 | 90.2704 | 80.5742 | 90.3482 | 88.5267 | 92.7075 | 82.5992 | 88.4744 | 81.6405 | 79.815 | 97.424 | 82.821 | 87.2487 | 84.5632 | 82.8792 | 94.0336 | 88.3426 | 73.939 | 81.5904 | 82.5809 | 95.2799 | 85.746 | 99.137 | 75.7943 | 83.4082 | 83.1003 | 90.7932 | 78.2121 | 89.5244 | 89.6487 | 93.5504 | 82.6152 | 78.5671 | 85.3707 | 90.8857 | 94.4674 | 80.1317 | 87.6415 | 78.1775 | 92.3723 | 95.0438 | 81.7272 | 77.988
M4 | 79.3962 | 92.5034 | 95.304 | 82.3909 | 78.1449 | 83.5503 | 81.9446 | 84.0613 | 92.4883 | 96.1402 | 80.0369 | 87.7403 | 85.4797 | 84.5185 | 92.1171 | 80.0547 | 90.751 | 89.824 | 94.0021 | 82.333 | 88.319 | 81.2104 | 80.2803 | 97.7417 | 83.5533 | 86.8613 | 85.1941 | 83.4664 | 94.2326 | 88.651 | 74.1476 | 82.3958 | 83.8718 | 95.3161 | 87.3348 | 100.833 | 76.9257 | 84.9913 | 83.6928 | 92 | 78.6347 | 90.619 | 90.894 | 93.9022 | 83.4124 | 80.7542 | 86.2285 | 92.7234 | 95.5221 | 80.6523 | 88.2791 | 79.904 | 93.9583 | 95.2272 | 81.3566 | 78.224
Arrangement of LED sources on the macroscopic system
Reproducibility of transmission ratio

## Slide 11: Experimental results – Compact PoC (1/3)
Shift to more compact prototype:
  OLED display replaces LEDs
  CMOS sensor replaces photodiodes
  Peripherals controlled by Raspberry Pi
Preliminary analyses:
  RAW values & sub-pixel control
Schematic sectional view
Photograph of the experimental set-up
PUF package
OLED module
Thin film
CMOS sensor

## Slide 12: Experimental results – Compact PoC (2/3)
Problems caused by changing components:
Chart: Comparison OLED mesured spectra with IMX219 Bayer filter from datasheet
Bayer filter pattern (BGGR)  Limit effect of thin film
Micro lens shifted on edges
 Crosstalk
Refresh rate + Exposure time
 Flickering phenomenon

## Slide 13: Experimental results – Compact PoC (3/3)
Comparison of results with TiO2 and LiNbO3:
 | Target | TiO2 | LiNbO3
Uniformity (%) | 50 | 51.4 | 48.7
Reliability (%) | 100 | 91.1 | 94.5
Uniqueness (%) | 50 | 48.5 | 45.0
LiNbO3
TiO2

## Slide 14: III. Outlook
Results confined to the experimental prototype to date
Several avenues for progress identified:
  Custom CMOS sensor
  FPGA/ASIC-based reader
  Simulation tools (noise, response discrepancy)
  Post-processing operations

## Slide 15: Thank you for your attention

## Slide 16: References
[1] Maiti, Abhranil, Vikash Gunreddy, et Patrick Schaumont. « A Systematic Method to Evaluate and Compare the Performance of Physical Unclonable Functions ». In Embedded Systems Design with FPGAs, édité par Peter Athanas, Dionisios Pnevmatikatos, et Nicolas Sklavos, 245‑67. New York, NY: Springer, 2013. https://doi.org/10.1007/978-1-4614-1362-2_11.
[2] Pappu, Ravikanth, Ben Recht, Jason Taylor, et Neil Gershenfeld. « Physical One-Way Functions ». Science 297, no 5589 (20 septembre 2002): 2026‑30. https://doi.org/10.1126/science.1074376.
[3] Guajardo, Jorge, Sandeep S. Kumar, Geert-Jan Schrijen, et Pim Tuyls. « FPGA Intrinsic PUFs and Their Use for IP Protection ». In Cryptographic Hardware and Embedded Systems - CHES 2007, édité par Pascal Paillier et Ingrid Verbauwhede, 63‑80. Lecture Notes in Computer Science. Berlin, Heidelberg: Springer, 2007. https://doi.org/10.1007/978-3-540-74735-2_5.
[4] Maes, Roel. Physically Unclonable Functions: Constructions, Properties and Applications. Physically Unclonable Functions: Constructions, Properties and Applications. Vol. 9783642413957, 2013. https://doi.org/10.1007/978-3-642-41395-7.
[5] Zhang, Shen, Bin Gao, Dong Wu, Huaqiang Wu, et He Qian. « Evaluation and Optimization of Physical Unclonable Function (PUF) Based on the Variability of FinFET SRAM ». In 2017 International Conference on Electron Devices and Solid-State Circuits (EDSSC), 1‑2. Hsinchu: IEEE, 2017. https://doi.org/10.1109/EDSSC.2017.8126474.
[6] Helfmeier, Clemens, Christian Boit, Dmitry Nedospasov, et Jean-Pierre Seifert. « Cloning Physically Unclonable Functions ». In 2013 IEEE International Symposium on Hardware-Oriented Security and Trust (HOST), 1‑6, 2013. https://doi.org/10.1109/HST.2013.6581556.

## Slide 17: Supplementary Information
Acquisitions without thin film
Calculate transmission factors
Analyze responses
Process exploiting local maxima of transmission factor
Acquisitions with thin film sample
Define responses
Challenge
  OLED pixel position
  Sub-pixel color
  Sensor pixel position
Response
  Binary value
Rescale
Smooth
Mask
Binarize